## Slide 1: MICROFLEX Project - Microtechnology in Smart Fabrics
Prof Steve Beeby EEE Research Group
CIMTEC 2012
12th June 2012
S Beeby, R Torah, K Yang, Y Wei, J Tudor
Electronics and
Computer Science
Notes: Please use the dd month yyyy format for the date for example 11 January 2008. The main title can be one or two lines long.

## Slide 2: Overview
Introduction to MicroFlex
Functional Inks Development
  Case Study 1: Printed heater on fabric
  Case Study 2: Printed strain gauge on fabric
  Case Study 3: Printed piezoelectrics on fabric
Mechanical Microstructures on Fabric
Conclusions

## Slide 3: Research at Southampton
ECS was founded over 60 years ago
100 academic staff (36 professors)
140 research fellows, 250 PhD students
Research grant income: > £12 million p.a.
Over 20 years experience in developing printable active materials
3 ongoing research projects on smart fabrics (2 more completed):
  Microflex (EU Integrated Project)
  Energy Harvesting Materials for SFIT (EPSRC)
  Fabric based medical device (Wessex Medical)
£100 million Mountbatten Building, housing state of the art cleanroom.

## Slide 4: MicroFlex Project
The MicroFlex Project is a EU FP 7 funded integrated project, 7.7 M€ Budget, 5.4 M€ funding.
4 Year project, end date 30th October 2012.
13 Partners, 7 industrial, 9 countries.
Develop MEMS processing capability for the production of flexible smart fabrics. Based on screen and inkjet printing.
Develop new functional inks to be compatible with fabrics.
Produce industrial prototypes demonstrating the functionality of the new inks.
http://microflex.ecs.soton.ac.uk

## Slide 5
5
Envisaged Process Flow
Screen printing
Curing
Ink jet printing
MEMs on fabric
Fabric
Functional inks
Lab trials
Design & simulation
Active material
Sacrificial layer removal process

## Slide 6: Example Functions and Applications
6
Mechanical action
Lighting
Sensor
Drug delivery
Medical
Transport
Workwear
Consumer
Smart bandage, auto sterilization uniform, active monitoring underwear
Luminous cabin, smart driver seat,
auto clean filters
Danger warning workwear (heating suite, high visibility, gas sensing, temperature sensing, movement sensing, alarm sounder
Massage and cooling/heating armchair, surroundings customisation

## Slide 7
Screen Printing
7
Substrate
Substrate
Substrate
Substrate
Mesh
Mask
Squeegee
a)
b)
c)
d)
ink
Also known as thick-film printing, this is normally used in the fabrication of hybridised circuits and in the manufacture of semiconductor packages.

## Slide 8: Inkjet Printing
Non contact direct printing onto substrate, used for fabrics and electronics applications.
http://spie.org/x18497.xml?ArticleID=x18497

## Slide 9: Functional Inks Development
Research underpinned by novel ink development
Inks need to be flexible, low temperature and robust
Numerous ink types are required:
Passive | Basic functional | Advanced functional
Interface layer | Conductive | Piezoresistive
Encapsulation layer | Dielectric | Piezoelectric
Structural |  | Electroluminescent
Sacrificial |  | Gas sensitive
 |  | Semiconducting

## Slide 10: Case Study 1: Printed Heater
Simple heater is a current carrying conductive element.
Existing heaters integrated in textiles by weaving or knitting.
Heated Car Seat element BMW (www.bmw.com)
Woven approach limited by direction of warp and weft.
Knitted solution requires specialist equipment .

## Slide 11: Interface layer
Overcomes surface roughness and pilosity of fabric substrate providing a continuous planar surface for subsequent printed layers.
Cross-section SEM micrograph of 4
screen printed interface layers on
polyester cotton fabric

## Slide 12: Heater Design
Heater printed on a fabric area of 10 x 10 cm.
Heater should be flexible and maintain the properties of the fabric as much as possible.
Chosen track width of 1 mm for good compromise between conduction and flexibility.
Heater area coverage should be a maximum of 50% of the fabric.
Total track length of 1651.5 mm.
Total area coverage for the heater = 1663.52 mm2.
Percentage coverage = 20.5%

## Slide 13: Screen Design
Heater has three layers: Interface, Conductor and Encapsulation.
Interface layer improves heater performance but increases fabric coverage to ~40% - still below limit of 50%.
Fabric
Interface layer
Conductor layer
Encapsulation layer
10cm
10cm
Interface screen
Conductor screen
Complete design

## Slide 14: Finished Print
Layers | Printed Thickness
Substrate | Polyester Cotton from Klopman
Interface (Fabink-UV-IF1) | ~120 µm
Conductor (ELX 30UV) | ~7 µm
Encapsulation (Fabink-UV-IF1) | ~40 µm
Interface layer
Conductor layer
Encapsulation layer

## Slide 15: Influence of Interface Layer
Printed track calculated sheet resistance for each substrate
Interface
Fabric
Alumina
Printed track on each
substrate
80 mΩ/sq
194 mΩ/sq
50 mΩ/sq

## Slide 16: Results
50 oC heating achieved with 30 V and current limit of 200 mA.
Increases to 120 oC after 15 minutes with 600 mA current limit.
Fabric temperature within 2% of track temperature.
Low pattern percentage ensures fabric remains flexible and maintains key fabric properties such as breathability and wearer comfort.

## Slide 17: Case Study 2: Strain Gauge
Printed strain gauge demonstrated by project partners Jožef Stefan Institute, ink developed by ITCF and fabric from Saati.
Exploits the piezoresistive effect: the resistance of a printed film changes as it is strained (stretched) due to a change in the resistivity of the material.
Useful for sensing movement, forces and strains.

## Slide 18: Printed Sensor
Silver electrodes printed using a low temperature polymer silver paste.
Piezoresistive paste is based on graphite.
Cured at 120-125 oC
1 print
2 prints
3 prints

## Slide 19: Results
Sensitivity illustrated by the Gauge factor:
Clear increase in resistance demonstrated as the fabric is strained.
Conventional metal foil GF = 2
N° of graphite layer | R0 (Ω) at 0 % strain | R(Ω) at 1.5 % strain | Gauge factor
1 | 1905 | 2064 | 5.6
2 | 1100 | 1198 | 5.9
3 | 328 | 358 | 6.1

## Slide 20: Strain vs Load
By measuring resistance the load on the fabric can be calculated.
B. Perc, et al. ‘Thick-film strain sensor on textiles’, 45th International Conference on Microelectronics, Devices and Materials - MIDEM, Slovenia 9-11 Sept 2009.

## Slide 21: Case Study 3: Piezoelectric Films
Piezoelectric materials expand when subject to an electrical field, similarly they produce an electrical charge when strained.
Ideal material for sensing and actuating applications.
Meggitt have developed a screen printable piezoelectric paste that can be printed onto fabrics.
http://www.piezomaterials.com

## Slide 22: Piezoelectric Structure
Piezoelectric material sandwiched between electrodes.
Polarising voltage required after printing to make the piezoelectric active.
Cured at temperatures below 150 oC.
Promising sensitivity demonstrated (d33 ~ 30 pC/N)
22
Images courtesy of Meggitt Sensing Systems

## Slide 23
23
Printed MEMS
The MicroFlex project is concentrating on fabricating sensors and actuators (transducers) and developing printed MEMS.
MicroFlex aims to use standard printing techniques and custom inks in order to realise freestanding mechanical structures coupled with active films for sensing and actuating.
Developed a surface micromachining process for printed films on fabrics

## Slide 24: Printed MEMS Process
Piezoresistive layer
Interface layer
Sacrificial layer
Structural layer
Fabric
Electrode
Sacrificial layer requirements: printable, solid, compatible, can be easily removed without damaging fabric or other layers.
Structural layer requirements: suitable mechanical/functional properties.

## Slide 25: Process Requirements
Implemented by screen printing.
Sacrificial technology: removal method must be compatible with fabrics i.e. low temperature, non solvent based.
Structural material and its processing must be compatible with the sacrificial material.
Structural materials properties chosen for the particular application.

## Slide 26: Example Structure
Capacitive Cantilever:
Sample 4 Sample 3 Sample 2 Sample 1
Sample 4 Sample 3 Sample 2 Sample 1
Sample 4 Sample 3 Sample 2 Sample 1
Sample 4 Sample 3 Sample 2 Sample 1
Sample 4 Sample 3 Sample 2 Sample 1
Interface layer
Bottom electrode layer
Sacrificial layer
Structural layer
Top electrode layer

## Slide 27: Sacrificial Material and Process
Plastic crystal (Trimethylolethane, TME):
  An intermediate solid form between the real solid and liquid forms
  Sublimation instead of liquefaction
Sublimation starts around 87 oC
Low curing and removal temperatures
  Curing: 80-85 oC
  Removal: 150-160 oC

## Slide 28: Results
Sacrificial layer was completely removed at 160 oC.
No visible damage to fabric properties
Chart: 1/L2 (m-2)
| 12345.679012345681
Sample 1 | 760
Sample 2 | 415
Sample 3 | 285
Sample 4 | 215
Line | 752.8042 | 433.0511 | 285.0511 | 204.656
Resonance test shows cantilever was fully undercut, and results match FEA.

## Slide 29: Piezoelectric Cantilever
Piezoelectric version also fabricated
Film thicknesses:
  Interface layer ~100 mm
  Sacrificial layer ~100 mm
  Structural layer ~80 mm
  Electrodes ~15 mm
  PZT 75-100 mm
Voltage versus frequency for different acceleration levels.

## Slide 30: Micropump
Initially printed on Kapton, demonstrates sacrificial process combined with structural, conductive and piezoelectric films.
Uses passive nozzle/diffuser valves, achieves 27 uL/min from 100 VP-P at 1 MHz, pumping IPA.
Chamber
Top electrode
Bottom electrode
PZT layer
Flow path

## Slide 31: Conclusions
MicroFlex has developed the materials and processes required to fabricate printed MEMS on fabrics.
Wide range of active inks have been developed.
Numerous prototypes based upon these active inks demonstrated.
Sacrificial layer fabrication process has also been demonstrated and is being applied to several structures and devices including accelerometers, pressure sensors and micropumps.

## Slide 32: Smart Fabric Inks Ltd
Company launched February 2011
Marketing inks developed at the University of Southampton
Please visit www.fabinks.com for further information

## Slide 33: Acknowledgements
Colleagues at Southampton, MicroFlex partners and EU for funding (CP-IP 211335-2).
  Thanks for your attention!